## Slide 1: Point Defects in Gallium Nitride (GaN) ---
Presented By: Md. Rayid Hasan Mojumder
Department of Engineering Science and Mechanics,
The Pennsylvania State University – University Park, PA, USA

## Slide 2: Outline
Introduction
Results and Discussion
Conclusion and Future Works

## Slide 3: Introduction
Background on GaN (hexagonal):
  Wide direct bandgap (~3.5 eV) – high power and high frequency
  High electron mobility (~2000 cm2/Vs)
  High breakdown voltage (~3.3 MV/cm)
  Doping – p type (Mg) and n type (Si)
  Applications – LEDs, lasers, power electronics, solar cells
Lyons et al., Appl. Phys. 129, 111101 (2021)
Freysoldt et al., Rev. Mod. Phys. 86, 253 (2014)
Freysoldt et al., Phys. Rev. Lett. 102, 016402 (2009)
Issues with GaN:
  Lower thermal conductivity (~1.3 W/cmK)
  MOCVD Growth issues - defects, unintentional contaminants, and impurities

## Slide 4: Introduction cntd.
Important defect properties in GaN:
1Yang et al., Sci. Rep. 6, 21712 (2016)
2Shinozuka, Jenny Stanford Publishing (2021)
Lyons et al., npj Comp. Mat. 3, 12 (2017)
Van der Walle et al., Appl. Phys. 95, 3851–3879 (2004)
Lyons et al., Appl. Phys. 129, 111101 (2021)
  Nonradiative (SRH) recombination centers1
  Deep donor level defects in III-V compound alloys – DX center2
(+) Trapping localized holes by acceptors – Polaronic
Decreased efficiency
Slower response times
Heat loss
Performance instability

## Slide 5: Introduction cntd.
Defect Investigation in GaN:
  Theoretical – DFT (point defects, impurities, deep defects)/MD (dislocations)
  Experimental – Photoluminescence (PL) and Deep Level Transient Spectroscopy (DLTS)
Reshchikov et al., J. Appl. Phys. 97, 061301 (2005)
Narita et al., AIP Pub. (2020)
Abou-Ras et al., Wiley-VCH (2016)
Formation energies for impurities, vacancies, and interstitials calculated and compared with literature
[VASP + PyDefect – PBE]
This work

## Slide 6
GaN Defect Investigation with PyDefect
Relaxed GaN Unit Cell –
a = b = 3.197 Å, c = 5.2 Å, BG = 1.8442 eV (PBE) – prev.
a = b = 3.219 Å, c = 5.242 Å, BG = 1.7 eV (PBE) – current
1a = b = 3.22 Å, c = 5.24 Å, BG = 1.71 eV (PBE)
2a = b = 3.22 Å, c = 5.22 Å, BG = 1.71 eV (PBE)
3a = b = 3.19 Å, c = 5.19 Å, BG = 3.51 eV (exp.)
1González-Hernández et al., App. Surf. Sci. 314, 794-799 (2014)
2Lyons et al., npj Comp. Mat. 3, 12 (2017)
3Vurgaftman et al., J. Appl. Phys. 94, 3675–3696 (2003)
Ga
N
a = b = 3.19 Å, c = 5.19 Å (materials project)
Hexgonal wurtzite, 4 atoms, 6 mm

## Slide 7
GaN Defect Investigation with PyDefect cntd.
GaN unit cell band diagram (BG = 1.7 eV)
GaN unit cell DOS and PDOS (BG = 1.7 eV)

## Slide 8
GaN Defect Investigation with PyDefect cntd.
Convex hall diagram
Chemical potential diagram
Fraction
Formation Energy (eV/atom)
Ga –Ga(bulk) = - 0.9 eV1
1Feenstra et al., J. Vac. Sci. Technol. B 23, 1174–1180 (2005)

## Slide 9
GaN Defect Investigation with PyDefect cntd.
Defect elements: vacancy, interstitials, and anti-sites
Ga_i1: [-1, 0, 1, 2, 3]
Ga_i2: [-1, 0, 1, 2, 3]
N_Ga1: [-6, -5, -4, -3, -2, -1, 0]
Va_Ga1: [-3, -2, -1, 0, 1]
N_i1: [-3, -2, -1, 0, 1]
N_i2: [-3, -2, -1, 0, 1]
Va_N1: [-1, 0, 1, 2, 3]
Ga_N1: [0, 1, 2, 3, 4, 5, 6]
Ga-rich
N-rich
Formation Energy Diagram

## Slide 10
GaN Defect Investigation with PyDefect cntd.
Defect elements: vacancy, interstitials, and anti-sites
Ga_i1: [-1, 0, 1, 2, 3]
Ga_i2: [-1, 0, 1, 2, 3]
N_Ga1: [-6, -5, -4, -3, -2, -1, 0]
Va_Ga1: [-3, -2, -1, 0, 1]
N_i1: [-3, -2, -1, 0, 1]
N_i2: [-3, -2, -1, 0, 1]
Va_N1: [-1, 0, 1, 2, 3]
Ga_N1: [0, 1, 2, 3, 4, 5, 6]
Ga-rich
N-rich
Formation Energy Diagram (extended to HSE BG = 3.45 eV)

## Slide 11: Results and Discussion cntd.
Comparative Analysis
(this work, BG = 1.7 eV)
(BG = 1.71 eV1)
1Lyons et al., npj Comp. Mat. 3, 12 (2017)

## Slide 12: Conclusion
Properties co-doping or p-n junction in GaN:
  Defect captures free e- capture
  Electrical and optical properties altered
Future considerations:
  GaN with vacancy, interstitials, antisites
  GaN with vacancy, interstitials, antisites and Si (n-type)
  GaN with vacancy, interstitials, antisites, and Mg (p-type)
  Other impurities:
    Shallow dopants:
      Donor dopants: Si, Ga, O
      Acceptor dopants: Mg
    Deep dopants:
      Cation-site acceptors: Zn, Cd, Be, and Ca
      C
      Rear earth dopants
    Unintentional – Fe, H, C

## Slide 13: Additional Works
Defect formation energy – DOPED package
Potential file generation – ML + AIMD

## Slide 14: Thank you all!
Q&A

## Slide 15: Backup slides
Copyright belongs to the respective sources, demonstrated purpose only

## Slide 16: Calculation of Lattice constants

## Slide 17: Reading Formation Energy Diagram

## Slide 18: Reading Formation Energy Diagram cntd.

## Slide 19: Reading Formation Energy Diagram cntd.

## Slide 20: Reading Formation Energy Diagram cntd.

## Slide 21: Reading Chemical Phase Diagram

## Slide 22: Reading Chemical Phase Diagram
N-rich, because poten of N is higher than of Ga
Ga-rich, because poten of Ga is higher than of N

## Slide 23: Reading Chemical Phase Diagram
In this diagram, the x-axis represents the chemical potential of Ga and the y-axis represents the chemical potential of N. The line connecting points A and B represents the set of chemical potentials where GaN is stable. To the right of the line (toward point A), the conditions are Ga-rich because the chemical potential of Ga is higher and that of N is lower. To the left of the line (toward point B), the conditions are N-rich because the chemical potential of N is higher relative to that of Ga.
Point A, located at the intersection of the x-axis and the GaN stability line, would represent the most Ga-rich conditions under which GaN is stable. At this point, the chemical potential of Ga is at its highest possible value without forming metallic Ga, and the chemical potential of N is at its lowest.
Point B, at the intersection of the y-axis and the GaN stability line, represents the most N-rich conditions under which GaN is stable. Here, the chemical potential of N is at its highest possible value without forming molecular N2, and the chemical potential of Ga is at its lowest.
The slope of the line is determined by the stoichiometry of GaN. For every point along this line, the sum of the chemical potentials of Ga and N equals the chemical potential of GaN. This line essentially is a graphical representation of the reaction: GaN (solid)↔Ga (solid or liquid)+12N2(gas)GaN (solid)↔Ga (solid or liquid)+21​N2​(gas)
So, if you're performing a calculation or an experiment under conditions where you're along this line but closer to point A, you would say you are under Ga-rich conditions. If you're closer to point B, then you're under N-rich conditions. This concept is key when predicting the types of defects and their concentrations during the growth of GaN crystals.